Engine Air Filter Testing

R2C tested engine air filters from multiple manufacturers to establish comparative data for the R2C manufactured product.

Each filter was identical in size. With the exception of the R2C filter, which was manufactured by R2C using normal production materials and methods of construction, the individual filters were obtained on the open market and were tested to the exact same standards in order to establish the following performance characteristics:

- Initial efficiency.

- Initial filter restriction.

- Cumulative efficiency.

- Dust holding capacity.

The following equipment and test protocol was used to establish the test results:

- The tests were performed on a SAE J726 air filter test stand located in R2C’s test facility by a qualified R2C Laboratory Technician under the supervision of the Laboratory Supervisor and Engineering Manager.

- Each filter was tested to the ISO 5011 air filter test standard using PTI Fine test dust. Each test was corrected for temperature, humidity and duct barometric pressure. The laboratory is in an environmentally stabilized facility.

- Air flow for each test was 400 scfm. The dust feed rate was 0.028 grams/cubic foot of air flow.

- Dust capacity was measured at a 10” wg increase in filter restriction above the initial restriction. Cumulative efficiency was also established at this point.